Melton Classics, Inc.

PlasterCastTM

PRE FABRICATED GLASS FIBER

REINFORCED GYPSUM COLUMNS AND FORMS

Section 09275

PART 1	GENERAL:

1.01		WORK COVERED:

Manufacturer of GRG (Glass Fiber Reinforced Gypsum) Forms

1.02		RELATED WORK IN OTHER SECTIONS:

A.	Light gauge metal framing.

B.	Veneer gypsum plaster.

C.	Gypsum board.

D.	Finishing glass fiber reinforced gypsum.

E.	Miscellaneous metals.

1.03		SUBMITTALS:

Samples and shop drawings to conform to Section 01200

A.	Samples:

Samples submitted as required by architect.

B.	Shop Drawings:

Submit shop drawings completely detailing prefabricated glass fiber 				reinforced gypsum members, including locations, sizes and shapes of 				members, proposed jointing arrangements, details of anchorages and 				supports, suspension systems, outlet boxes, and other items which occur in or are affected by prefabricated gypsum members shall be prepared at the factory by manufacturer only for those items indicated on approved shop drawings.

1.04		STANDARDS OF PERFORMANCE, DESIGN AND QUALITY:

A.	Manufactures Qualifications:

Melton Classics, Inc. has a demonstrated capability to produce GRG 				products of the quality and scope required for any project.

B.	All GRG forms shall match approved samples.

C.	All GRG forms will be installable according to details submitted in shop 				drawings.

PART 2	PRODUCTS:

2.01		MANUFACTURER:

Melton Classics, Inc.

P.O. Box 465020

Lawrenceville, GA  30042

(770) 963-3060  (800) 963-3060  Fax: (770) 962-6988

2.02		MATERIALS:

A.	Description:	Glass Fiber Reinforced Gypsum (GRG)

1.	Pre molded GRG parts are fabricated to details and dimensions 					shown.

2.	Finished product shall conform to the following standards.

PHYSICAL PROPERTIES OF GRG "FIBROCAL"

a.	Shell Thickness:

3/16" minimum except for small components which may be 					1/8" minimum, large components such as wall panels shall 						be of the thickness recommended by the manufacturer for 						the size and location of components.

b.	Weight: 1.5 lbs. per square foot

c.	Flexural Strength: 4,192 psi

d.	Tensile Strength: 1,340 psi

e.	Compressive Strength: 5,800 psi

f.	Density: 110 lbs. per cubic foot

g.	Hardness (Barcol): 105

h.	Flammability:

Flame Spread		0

Smoke Developed	0

ASTM E4		Class A

i.	Glass Content: 38.7%

3.	All parts to contain supports as required to keep within allowable 					tolerances.

4.	Finish surfaces shall be true or textured according to design 					requirements.

2.03		FABRICATION:

A.	Molds to be constructed of reinforced fiberglass to produce units 					conforming to the required profiles, dimensions and tolerances.

B.	Allowable Tolerances:

1.	Dimensional Tolerances: + 1/8"

2.	Wall Thickness: Nominal 3/16"

3.	Out of Plumb: + 1/8"

4.	Bowing: L/360 Maximum

PART 3	EXECUTION

3.01		INSTALLATION

A.	General:

Employ only workmen experienced, skilled and trained on this type of 				quality erection work.

B.	Workmanship:

Install work of this section complete, straight, plumb, level, in true 					alignment and securely anchored.

C.	Erection:

GRG forms shall be installed per drawings, including the approved shop 				drawings, and the manufacturer's written recommendations and instruction 			for this project.

D.	Sealing and Caulking:

Shall conform to requirements of Caulking and Sealing Section 07900 and 			requirements indicated and specified herein.

1.	Joints and Sealants: Joints (quantity, sizes, and shapes) indicated 					on contract drawings are minimum requirements.

E.	Finishing Materials:

1.	Fasteners:

As indicated on approved shop drawings and in accordance with 					manufacturer's printed recommendations.

2.	Joint treatment materials:

a.	General: ASTM C-475; type recommended by the 							manufacturer for the application indicated, except as 						otherwise indicated.

b.	Joint tape: Perforated type.

c.	Joint Compound: Ready Mixed vinyl-type for interior use.

(1) Grade: 2 separate grades; one specifically for bedding 						tapes and filling depressions, and one for topping and 						sanding.

3.	Miscellaneous Materials:

a.	General: Provide auxiliary material for work of types and 						grades recommended by manufacturer.

b.	Adhesive: Special adhesive recommended for laminating 						gypsum plaster.

F.	Replacements:

1.	In-place GRG forms may be rejected for the following 						reasons.

a.	Nonconformance to detail requirements specified 							previously.

b.	Nonconformance with approved samples.

c.	Nonconformance to specified fabrication or installation 						tolerance.

d.	Damage beyond satisfactory field repair, as determined by 						the Architect.

3.02		CLEANUP:

General:

Perform cleaning procedures as recommended by GRG unit manufacturer.

3.03		GUARANTEE:

One year from substantial completion.